## Slide 1: Standalone stretchable device platform for human health monitoring
Larry Cheng, Associate Professor at Penn State
Huanyu.Cheng@psu.edu
Notes: Standalone stretchable device platform for human and structural health monitoring
Dissolvable Tattoo Electronics for Biomedicine
Deformable Multimodality Sensors

## Slide 2
acknowledgements

## Slide 3
The Persistence of Memory, Salvador Dalí, 1931
Soft Approach to Electronics

## Slide 4: Device-interconnect Design
SIDE VIEW
Elastomer
TOP VIEW
Interconnects
Electronics
Microscale stretchable battery :
  >300% biaxially, little loss over cycles
Mechanically robust construction for repeatable use:
Bi-layer substrate
Top: soft -> stretchable
Bottom: stiff -> high strength
Nat. Commun. 4, 1543 (2013)
Adv. Mater. 25, 6839 (2013)

## Slide 5
Stretchable LEDs
Nano Lett. 11, 3881 (2011)
Temperature sensors
Nat. Mater. 12, 938 (2013)
Adv. Funct. Mater. 24, 3846 (2014)
Hydration and strain
Small 11, 906 (2015)
Near field communication
Fingertip electrode
Nanotechnology 23, 344004 (2012)
Various stretchable Sensors

## Slide 6
Integrated system
3 cm
EOG sensor
EEG sensor
Color changeable glass
Wireless integrated circuit (Acceleration sensor, Ultraviolet sensor)
ACS Appl. Mater. Interfaces 12, 21424 (2020)
Smart electronic eyeglasses
Bioelectronic complex on the urinary bladder
Sci. Adv. 6, abc9675 (2020)
NPG Asia Mater. 12, 17 (2020)
NOx gas sensor
3D integumentary membrane on heart
Nat. Commun. 5, 3329 (2014)

## Slide 7
precision medicine and healthy aging

## Slide 8
Research thrusts
Low-cost manufacturing approaches
Standalone stretchable device platform
Nanomaterial composites
3D freeform fabrication
Standalone device
Body area network
Nanomaterial composite
10 μm
LIG/Ni/Au

## Slide 9
Trends Analyt. Chem. 133, 116085 (2020)
Stretchable gas sensors
Application:
Health biomarker
Industry safety
Environmental monitoring
Military countermeasures

## Slide 10
LIG sensing platform
Drop cast
sensing materials
Coat Ag ink
on serpentine
(i)
(ii)
Transfer LIG/PI to soft substrate
Self heating
Dispersing sensing material precursors before laser writing
Femtosecond, UV or CO2 laser
Skin-conforming
J. Mater. Chem. A 8, 6487 (2020) (Cover)
20 μm
Porous LIG
NO2
6
4
2
0
Response (‰)
1 ppm
100 ppm
Ammonia
Acetone
Ethanol
Methanol
rGO/MoS2 @60ºC
1 ppm
1 ppm
SO2
CO
NO
NO2
Ammonia
Ethanol
Methanol
Acetone
1 ppm
1 ppm
100 ppm
Response (‰)
0
1
-1
-2
2
CuO/ZnO @RT
Varying gas specificity for combinatorial sensing

## Slide 11
LIG functional composites
Breathable gas sensor
ACS Appl. Mater. Interfaces 14, 17818 (2022)
VOx-doped LIG to decouple NOx and T
NO
NO
NO
NO2
NO2
VOX-doped LIG
Unpublished
Chem. Eng. J. 444, 136631 (2022)
Dual-mode for T and subtle motion
Microsyst. Nanoeng. 8, 78 (2022)
With semi-permeable membrane for moisture-resistant gas sensing
asthma or COPD
Breath analysis

## Slide 12
LIG glucose sensor
0
4
2
6
Glucose concentration (mM)
Current density (mA/cm2)
0
4
8
12
LIG foam
LIG fiber
LIG foam
LIG fiber
ⅰ
ⅱ
LIG90/AgNW5
LIG
ⅲ
ⅳ
PDMS
PI
LIG
CO2 laser
Nickel
Au
Laser scribing
Nickel plating
Gold plating
Assembly
RE
CE
WE
PDMS
Glucose sensor
Cavity
Porous
Ecoflex
LIG/Ni_3/Au
Biosensors and Bioelectronics 193, 113606 (2021)
Arm
Top
Side
Bottom

## Slide 13
  Substrate: Silk (FDA approved), PLGA
  Interconnects: Mg, Fe, Zn, W
  Electronic components: Si, SiO2
Transient Electronics
Rec. Daily Intake
Electronics that dissolve
Science 28, 1640 (2012) (Cover);
Adv. Mater. 26, 1992 (2014); Adv. Funct. Mater. 24, 645 (2014)
Mg ~ 300 mg, Si ~ 10 mg
Mg ~ 100 mg, Si ~ 3 mg

## Slide 14
MgO: thickness control
Silk: tunable dissolution
Time (hr)
R/L (Ω/mm)
0
20
10
30
0
120
80
100
10
5
Silk overcoat
MgO
Mg
ACS Appl. Mater. Interfaces 7, 19870 (2015)
Science 28, 1640 (2012) (Cover)
Engineered Lifetime

## Slide 15
Mg/MgO
inductor
Mg/MgO
capacitor
Mg resistor
Si/MgO/Mg
transistor
Si diode
Mg interconnect
2mm
silk
5 min
3 min
10 min
In water
0 min
1 cm
Science, 2012, 28, 1640 (Cover)
System Level Device

## Slide 16
Nature, 2016, 530, 71
Nat. Mater. 15, 782 (2016)
Brain monitor
Cerebral cortex spatiotemporal mapping
Transient implantable devices
3.5
4.0
4.5
5.0
0.9
0.6
0.3
0.0
-0.3
Zn
Voltage (mV)
Time(s)
0.9
0.6
0.3
0.0
-0.3
Gel
3.5
4.0
4.5
5.0
Voltage (mV)
Q
R
S
T
Q
R
S
T
ACS Appl. Mater. Interfaces 10, 36664 (2018)
Low-cost transient sensors

## Slide 17
Large scale AM w/ xenon flash
J. Mater. Chem., 2012, 22, 15683
Large-scale, Roll-to-Roll
Intense pulsed light sintering
Nanotechnology, 2016, 27, 495602
Broad oFutput spectra
Fast and high energy (1000J within ms)
Small, 2017, 13, 1700065
Wide range of materials
Conductors (Zn NPs, Ag NPs/NWs/film, Au, Cu)
Semiconductors (indium gallium zinc oxide, IGZO; Cu2ZnSnS4, CZTS)
On diverse substrates (glass, plastic, polymer)

## Slide 18
3D biodegradable sensors
Materials Today 50, 24-34 (2021) (Front Cover)
i
ii
iii
iv
v
1 μm
1 μm
AgNO3
CuSO4

## Slide 19
3D biodegradable sensors
Smart Internet-of-Things (IoTs)
Dipole antenna
Electrodes
Hydration sensor
Temperature sensor
Temperature sensor
0
5
10
15
Time (min)
20
40
60
Temperature ( ̊ C)
hot water
cold water
empty beaker
40
50
60
70
Relative Humidity (RH)
80
-25
-30
-35
ΔR/R (%)
-40
-45
1st
2nd
-40
-30
-20
S11 ( dB)
2
3
4
5
-10
Frequency (GHz)
0
No water
Contacting
Immerged
Humidity sensor
Dipole antenna
Materials Today 50, 24-34 (2021) (Front Cover)
i
2cm
glass
ii
2cm
PS
iii
2cm
PET
iv
2cm
PI

## Slide 20
Circuits on complex seashell
50 μm
10 μm
1cm
20 μm
5 μm
1cm
Zn layer patterned on the seashell
Ag layer on the seashell by a single-replacement reaction
Materials Today 50, 24-34 (2021) (Front Cover)

## Slide 21
Body area sensor network
ACS Appl. Mater. Interfaces 12, 45504 (2020)
On-body sensors
Antenna
FPCB

## Slide 22
Simple fabrication process
Reduced roughness
50 μm
25 μm
Before
After
sintering aid layer
Antenna
Flexible printed circuit board (FPCB)
3D origami paper structures
Interfacial sintering at room temperature
R
180◦
800 nm
Sintering aid layer
Ag
paper
< 1μm
Stamping on the textured skin surface
Drying with hairdryer

## Slide 23
On-body sensors
98.7 %
95.2 %
99 %
95 %
Exercise
1 min
Our sensor
Commercial pulse oximeter
Rest
After exercise
Sample
Calibration
R2=0.9894
Temperature sensors
initial
29.0 %
87.0 %
99.7 %
5s blowing
10s blowing
1 min wait
Activity
20 Hz
1 kHz
10 kHz
2 MHz
Hydration sensors

## Slide 24
enhanced contact quality
10%
15%
commercial
Impedance
a
b
c
d
P
Q
R
S
T
U
20 Hz filter
e
Main frequency
ECG

## Slide 25
31
32
33
34
35
11
12
13
14
10
0
12
24
36
Time (s)
Commercial
Stretch
Compress
Magnitude (a.u.)
Our sensor
Motion artifact-free sensing
ECG/EMG
pH/glucose
Electrical Stimulation
Drug delivery
0
15
30
45
Time (s)
Magnitude (a.u.)
Dry
Wet
Unpublished

## Slide 26
Easy removal of sensors
(i)
(ii)
(iii)
(iv)
(i)
(ii)
(iii)
2 h at 25 °C
10 mins at 60 °C
5 mins at 60 °C
+ Stirring
Removal of the device from the skin in warm water flow
ACS Appl. Mater. Interfaces 12, 45504 (2020)

## Slide 27
Biosens. Bioelectron. 168, 112569 (2020)
Future perspective
Self-powered
Wireless

## Slide 28
Nano Energy 81, 105609 (2021)
self-powered stretchables
Stretchable ZnP@LIG supercapacitor

## Slide 29
Standalone Stretchable Sys.
Appl. Phys. Rev. 9, 011413 (2022), Cover
Pulse sensor powered by the self-charging units
Supercapacitor
Strain Sensor
Nano Energy 96, 107069 (2022)
RF charging

## Slide 30
Thank You for Your Attention!
LIG composites
Body area sensor network
3D freeform fabrication
Physiological signals
Standalone stretchable platform